# Medieval and post-medieval ceramic building materials fabrics: dating

July 2007

NB Please note these dates are continually been revised. Certain fabric types have, as yet, no secure date and are therefore excluded. Other features, such as the presence and absence of glaze can be used to refine the broad dates given here.

| Fabric | Earliest date (approx) | Latest date (approx) | Brief description |
| --- | --- | --- | --- |
| 2271 | 1180 | 1800 | local roofing tile |
| 2272 | 1135 | 1220 | early shelly roofing tile |
| 2273 | 1120 | 1220 | early sandy roofing tile |
| 2274 | 1080 | 1350 | finial and louver London ware pottery fabric |
| 2276 | 1480 | 1800 | fine moulding sand roofing tile |
| 2277 | 1200 | 1480 | local roofing tile |
| 2278 | 1200 | 1480 | non-local (Kent?) roofing tile |
| 2279 | 1630 | 1850 | pantile |
| 2537 | 1240 | 1450 | black iron oxide roofing tile |
| 2586 | 1180 | 1800 | local roofing tile |
| 2587 | 1240 | 1450 | black iron oxide roofing tile |
| 2816 | 1200 | 1800 | local roofing tile |
| 3062 | 1200 | 1800 | non-local? roofing tile |
| 3090 | 1200 | 1800 | black iron oxide roofing tile |
| 3091 | 1200 | 1800 | non-local? roofing tile |
| 3094 | 1200 | 1800 | sandy/black iron oxide roofing tile/pantile |
| 3097 | 1200 | 1800 | calcium carbonate (Kent?) roofing tile |
| 3201 | 1200 | 1800 | calcium carbonate (Kent?) roofing tile |
| 3204 | 1200 | 1800 | silty non-local? roofing tile |
| 3205 | 1200 | 1800 | very silty non-local? roofing tile |
| 3216 | 1200 | 1800 | very fine sandy roofing tile |
| 3228 | 1135 | 1200 | early sandy roofing tile |
| 3233 | 1200 | 1800 | 17th-century kiln furniture |
| 3234 | 1200 | 1800 | 17th-century kiln furniture/roofing tile |
| 3243 | 1270 | 1400 | yellow and pink non-local roofing tile |
| 2275 | 1630 | 1850 | pantile |
| 3085 | 1630 | 1850 | pantile |
| 3202 | 1630 | 1850 | pantile |
| 3203 | 1630 | 1850 | pantile |
| 3225 | 1630 | 1850 | pantile |
| 2280 | 1600 | 1900 | semi-circular drain |
| 2281 | 1700 | 1950 | circular drain |
| 2308 | 1470 | 1650 | stove tile |
| 2309 | 1470 | 1650 | stove tile |
| 2310 | 1470 | 1650 | stove tile |
| 3098 | 1470 | 1650 | stove tile |
| 3099 | 1470 | 1650 | stove tile |
| 1819 | 1520 | 1660 | tin-glazed floor tile |
| 2186 | 1520 | 1660 | tin-glazed floor tile |
| 2187 | 1520 | 1660 | tin-glazed floor tile |
| 2189 | 1520 | 1660 | tin-glazed floor tile |
| 2196 | 1520 | 1660 | tin-glazed floor tile |
| 2197 | 1520 | 1660 | tin-glazed floor tile |
| 3064 | 1520 | 1800 | tin-glazed tile |
| 3064F | 1520 | 1660 | tin-glazed floor tile |
| 3064W | 1630 | 1930 | tin-glazed wall tile |
| 3067 | 1520 | 1800 | tin-glazed tile |
| 3067F | 1520 | 1660 | tin-glazed floor tile |
| 3067W | 1630 | 1930 | tin-glazed wall tile |
| 3078 | 1520 | 1800 | tin-glazed tile |
| 3078F | 1520 | 1660 | tin-glazed floor tile |
| 3078W | 1630 | 1930 | tin-glazed wall tile |
| 3079 | 1520 | 1800 | tin-glazed tile |
| 3079F | 1520 | 1660 | tin-glazed floor tile |
| 3079W | 1630 | 1930 | tin-glazed wall tile |
| 3086 | 1520 | 1800 | tin-glazed tile |
| 3086F | 1520 | 1660 | tin-glazed floor tile |
| 3086W | 1630 | 1930 | tin-glazed wall tile |
| 3240 | 1520 | 1660 | tin-glazed floor tile |
| 3214 | 1520 | 1800 | tin-glazed tile |
| 3030 | 1400 | 1660 | brick |
| 3031 | 1350 | 1450 | Flemish-type yellow brick |
| 3032 | 1666 | 1900 | local post-Fire red brick |
| 3033 | 1450 | 1700 | local red `Tudor’ type brick |
| 3034 | 1666 | 1900 | local post-Fire red brick |
| 3035 | 1770 | 1940 | Kent yellow `stock’ brick |
| 3036 | 1600 | 1800 | small Dutch paving brick |
| 3037 | 1400 | 1660 | brick |
| 3038 | 1850 | 1950 | machine-made brick |
| 3039 | 1450 | 1700 | local red `Tudor’ type brick |
| 3040 | 1350 | 1450 | Flemish-type grass-marked brick |
| 3041 | 1360 | 1400 | brick |
| 3042 | 1400 | 1900 | local red `Tudor’ type brick |
| 3043 | 1270 | 1400 | Flemish-type estuarine silt brick |
| 3044 | 1300 | 1330 | yellow and red mottled brick |
| 3045 | 1270 | 1350 | brick |
| 3046 | 1450 | 1700 | local red `Tudor’ type brick |
| 3047 | 1700 | 1900 | brick |
| 3065 | 1450 | 1700 | local red `Tudor’ type brick |
| 3071 | 1400 | 1900 | brick |
| 3073 | 1400 | 1900 | brick |
| 3093 | 1380 | 1400 | brick |
| 3206 | 1450 | 1700 | red `Tudor’ type brick |
| 3208 | 1600 | 1800 | brick |
| 3209 | 1800 | 1900 | brick |
| 3211 | 1400 | 1900 | brick |
| 3210 | 1400 | 1660 | brick |
| 3214 | 1400 | 1900 | brick |
| 3215 | 1400 | 1900 | brick |
| 3217 | 1400 | 1900 | brick |
| 3218 | 1400 | 1900 | brick |
| 3219 | 1400 | 1900 | brick |
| 3220 | 1850 | 1950 | machine-made brick |
| 3221 | 1400 | 1900 | brick |
| 3222 | 1400 | 1900 | brick |
| 3223 | 1400 | 1900 | brick |
| 3224 | 1400 | 1900 | brick |
| 3235 | 1400 | 1900 | brick |
| 3242 | 1400 | 1900 | brick |
| 1810 | 1350 | 1390 | Penn floor tile |
| 2194 | 1300 | 1500 | floor tile |
| 1813 | 1300 | 1500 | floor tile |
| 2892 | 1250 | 1300+ | `Westminster’ floor tile |
| 2324 | 1300 | 1500 | floor tile |
| 2505 | 1300 | 1550 | floor tile, can be Flemish |
| 2320 | 1300 | 1500 | floor tile |
| 2316 | 1300 | 1500 | floor tile |
| 1811 | 1350 | 1390 | Penn floor tile |
| 2322 | 1300 | 1500 | floor tile |
| 2894 | 1350 | 1390 | Penn floor tile |
| 3066 | 1300 | 1500 | floor tile |
| 3084 | 1300 | 1500 | floor tile |
| 2199 | 1250 | 1300+ | `Westminster’ floor tile |
| 2195 | 1250 | 1300+ | `Westminster’ floor tile |
| 2851 | 1300 | 1500 | floor tile |
| 2317 | 1300 | 1500 | floor tile, can be Flemish |
| 3081 | 1250 | 1300+ | `Westminster’ floor tile |
| 3092 | 1060 | 1100 | Norman wall tile |
| 3241 | 1375 | 1405 | French Dieppe group floor tile |
| 2318 | 1450 | 1800 | silty Flemish floor tile |
| 2318E | 1450 | 1600 | glazed silty Flemish tiles |
| 2318L | 1600 | 1800 | unglazed Flemish tiles |
| 1977 | 1450 | 1800 | silty Flemish floor tile |
| 1977E | 1450 | 1600 | glazed Flemish tiles |
| 1977L | 1600 | 1800 | unglazed Flemish tiles |
| 2850 | 1450 | 1800 | silty Flemish floor tile |
| 2850E | 1450 | 1600 | glazed Flemish tiles |
| 2850L | 1600 | 1800 | unglazed Flemish tiles |
| 3063 | 1450 | 1800 | silty Flemish floor tile |
| 3063E | 1450 | 1600 | glazed Flemish tiles |
| 3063L | 1600 | 1800 | unglazed Flemish tiles |
| 3075 | 1450 | 1800 | silty Flemish floor tile |
| 3075E | 1450 | 1600 | glazed Flemish tiles |
| 3075L | 1600 | 1800 | unglazed Flemish tiles |
| 3076 | 1350 | 1390 | Penn floor tile, can also be Flemish |
| 3080 | 1450 | 1800 | silty floor tile |
| 3080E | 1450 | 1600 | glazed Flemish tiles |
| 3080L | 1600 | 1800 | unglazed Flemish tiles |
| 3082 | 1450 | 1800 | silty Flemish floor tile |
| 3082E | 1450 | 1600 | glazed Flemish tiles |
| 3082L | 1600 | 1800 | unglazed Flemish tiles |
| 1678 | 1300 | 1550 | calcium carbonate Flemish floor tile |
| 2497 | 1300 | 1550 | calcium carbonate Flemish floor tile |
| 2191 | 1300 | 1550 | calcium carbonate Flemish floor tile |
| 2504 | 1300 | 1550 | calcium carbonate Flemish floor tile |
| 2323 | 1300 | 1550 | calcium carbonate Flemish floor tile |
| 3083 | 1300 | 1550 | calcium carbonate Flemish floor tile |
| 1158 | 1300 | 1500 | floor tile |
| 3087 | 1500 | 1800 | post-medieval? floor tile |
| 2292 | 1500 | 1530 | Spanish cuenca floor tile |
| 3232 | 1300 | 1800 | floor tile, probably Flemish |
| 3213 | 1300 | 1800 | floor tile |
| 3274 | 1700 | 1950 | brick |
| 3275 | 1850 | 1950 | refractory brick |
| 3274 | 1850 | 1950 | refractory brick |